## Slide 1
Moose Logistics, LLC is the JV Partner and
Distributor for Great Façade Material to the USA
Metal Composite Panel
FR A class

## Slide 2
Company Introduction
ALUBOND （Jiangsu）is a JV company between USA and China investment.
ALUBOND(Jiangsu) mainly develop and manufact metal composite panel for building material & other application.
01

## Slide 3
标题文字添加
Factory view
ALUBOND(Jiangsu) had the full facility for metal composite panel which including manufacturing and further process. metal composite panel is available for international business.

## Slide 4
metal skin文字添加
02
Shape : It is two metal skin with mineral core bonded sandwich panel which is non-combustible system.
FR performance: It is a FR A class level composite panel which no limit for height or application area.
Mineral core文字添加
metal skin文字添加
Product introduction

## Slide 5
Al composite：paint coating（general solid color, metallic color, high gloss , prismatic etc), artificial paint color: (wood、stone 、cement etc）、anodizing (low gloss, high gloss); film(interior, exterior)
Stainless steel composite：sand, mirror, brush ,color
Ti-zinc composite ：blue gray、deep gray
Copper composite：red copper, brass (nature or aged)
TI composite：pure Ti
03
Surface Selection

## Slide 6
Pattern : It is not only metal type and color with many options. There are also many type of patterns available . Please contact us for color chart.

## Slide 7
Options
Green
Shape
Durability
Light
Non combustible
flame retardant
Super flat
Big size
2000*8000 available
Color consistencity
Super flat
Flame retardant
Color
impact
Big size
Economy
04
Typical Characteristics

## Slide 8
标题文字添加
标题文字添加
Non-combustible, no fire risk
Stay over >1200 C high temperature
Better performance than solid Al panel
Meet : ASTM E119-12, 2 hours fire resistance
Advantages：---FR A class，non-combustible and Flame retardant

## Slide 9
Composite panel make different curve shape reach a good result
Curve shape by composite panel

## Slide 10
4mm composite panel
3mm solid panel
Compare between solid panel and composite panel

## Slide 11
3mm solid panel make VMU
4mm composite panel make same VMU
Compare between solid panel and composite panel

## Slide 12
3mm solid panel
4mm composite panel
Compare between solid panel and composite panel

## Slide 13
Characteristics：
thickness：4mm
FR class：FR A2
top skin：0.5mm cooper+coating
core：mineral
bottom skin：coated 0.7mm AL skin
Specification：(limited by copper coil width)
Standard size：980mm*3200mm
Max size：980mm*7000mm
Substrate: red cooper, brass
05
Typical process—
Take copper composite panel as sample

## Slide 14
Original state of copper material changes until a stable surface is formed.
For example, the variation of red copper over time in the above figure.
At present, with the progress of materials science, we can pre oxidize copper in advance to achieve the desired color during the copper change process. Through coating protection measures, the appearance effect is relatively fixed for a period of more than 10 years.
As option, we could also offer original copper or brass as the skin to present the nature change .

## Slide 15
Brief of process – copper composite panel making
Original copper coil be handled by clean and pretreatment process make it ready for bonding.

## Slide 16
Original brass coil be handled by clean and pretreatment process make it ready for bonding. Then put coil through composite machine.

## Slide 17
Brass coil be loaded through composite machine bonding with core and bottom skin by high temperature and high pressure.

## Slide 18
Bonded panel go through cooling and flatting and cutting then be put as pallet.

## Slide 19
Lay the sheet on CNC table ready for groove and cutting
Pallet of the made sheets

## Slide 20
After folding and bending ,and put the bearing bar and hook put ready for package.
Collect the grooved sheets pass to folding and bending process

## Slide 21
Take off the protective film to check the surface color and quality
Take off the protective film to check the surface color and quality

## Slide 22
Install the sheets on building

## Slide 23
The pre- factory aging effect of copper is a chemical reaction process, and it is very difficult to maintain the consistency of appearance color. Usually, the final formed appearance has a certain color difference。 --world expo museum. Shanghai.

## Slide 24
The pre-factory aging effect of copper is a chemical reaction process, and it is very difficult to maintain the consistency of appearance color. Usually, the final formed appearance has a certain color difference。 --Super Intelligence Center, Shanghai

## Slide 25
characteristics：
thickness：4mm
FR class：FR A2
top skin：0.3mm stainless steel
core：mineral
bottom skin：coated 0.5mm AL skin
specification：(limited by SS coil width)
Standard size：1200mm*3200mm
Max size：1200mm*7000mm
Substrate: brush coil, sand coil, mirror 304,316 etc
Stainless steel composite panel
06

## Slide 26
black brush stainless steel panel for Union Pay
Mirror for Rizhao international center

## Slide 27
characteristics：
thickness：4mm
FR class：FR A2
top skin：0.5mm PVDF coil coating Al skin
core：mineral
bottom skin：coated 0.5mm AL skin
specification：(general coating, such as solid color, metallic color, prismatic color etc)
Standard size：1250mm*3200mm
Max size：2000mm*8000mm
Substrate: 3003 ,5005 etc alloy
Al coil coating composite panel-general
07

## Slide 28
GRAY PVDF coating for JAGUAR
SILVER PVDF coating for PROSCHE

## Slide 29
high gloss glass appearance metal panel fix on wall
Glass appearance metal panel

## Slide 30
characteristics：
thickness：4mm
FR class：FR A2
top skin：0.5mm PVDF coil coating Al skin
core：mineral
bottom skin：coated 0.5mm AL skin
specification：(artificial coating, such as wood, stone,cement color)
Standard size：1250mm*3200mm
Max size：1500mm*8000mm
Substrate: 3003 ,5005 etc alloy
Al coil coating composite panel-artificial
08

## Slide 31
stone – low gloss
Stone-high gloss

## Slide 32
wood –low gloss with sand pattern
texture available

## Slide 33
cement with texture
Texture

## Slide 34
characteristics：
thickness：4mm
FR class：FR A2
top skin：0.5mm anodized Al skin
core：mineral
bottom skin：coated 0.5mm AL skin
specification：(low gloss,high gloss, brush,sand,satin,mirror etc)
Standard size：1250mm*3200mm
Max size：1500mm*8000mm
Substrate: 3003 ,5005 etc alloy
Al anodized composite panel
09

## Slide 35
04
Anodized Al skin it is a high durability protect façade material, it is excellent performance especially under the tough environment such as close to sea, industrial area. The surface is harder than coating by reach a 9H pencil hardness. Also it is easy to clean due to the protection lay. Many color and type of gloss is available, please contact for color chart

## Slide 36
标题文字添加
Please contact us at uetmoose@yahoo.com
Or harry.wu.